## Slide 1: Reasons of crystallite formation during the GaAs nanowire self-catalyzed growth: Monte Carlo simulation
A.G. Nastovjak1, N.L. Shwartz1,2, E.A. Emelyanov1, M.O. Petrushkov1,
1 Rzhanov Institute of Semiconductor Physics, SB RAS, 13 Lavrentiev aven., 630090, Novosibirsk, Russia
2 Novosibirsk State Technical University, 20 K. Marx aven., 630073, Novosibirsk, Russia

## Slide 2: Semiconductor nanowires
Oehler, F. et. al, Nano Lett., 2018, 18, 701-708
GaP
Preobrazenskii V.V,, Putyato M.A, Emelaynov Е.А., Petrushkov М.О. (ISP SB RAS)
GaAs
Si
R. Dujardin, et. Aa. APL, 89, 153129 (2006) P. 1-3

## Slide 3: Vapor-liquid-solid growth of AIIIBV nanowires
Morral A., IEEE journal of selected topics in quantum electronics, 2011, 17, 819 -828
Self-catalyzed growth

## Slide 4: Experiment description
GaAs
Oxide removing, buffer deposition

## Slide 5
GaAs
Si deposition
Si
2.7 nm
GaAs
Oxide removing, buffer deposition
VgrSi = 0.014 ML/s
Ts = 410°С, PAs< 1·10-10 Torr
Experiment description

## Slide 6
Ga
GaAs
Si deposition
Si
2.7 nm
GaAs
GaAs
SiO2
Si
0.5 nm
Oxide removing, buffer deposition
VgrSi = 0.014 ML/s
Ts = 410°С, PAs< 1·10-10 Torr
tox = 40 min
Experiment description
As2
Si oxidation in airlock MBE chamber (T=300 K)

## Slide 7
Ga
As2
GaAs
Si deposition
Si
2.7 nm
GaAs
GaAs
Si oxidation in airlock MBE chamber (T=300 K)
SiO2
Si
0.5 nm
Oxide removing, buffer deposition
VgrSi = 0.014 ML/s
Ts = 410°С, PAs< 1·10-10 Torr
NW growth
GaAs
SiO2
Si
GaAs
Ga
T = 620° C
FAs4/FGa = 20
FGa = 0.23 ML/s
Experiment description
tox = 40 min

## Slide 8
Problem statement
GaAs(111)B
tgr = 15 min
L ~ 1 mm, d ~ 30 nm.
NW density ~2·107 cm-2
1 mm
Massive GaAs crystallites form between GaAs NWs
F.Bastiman et al, Nanotechnology 27, 095601 (2016)
F. Matteini et al. Cryst. Growth Des., 16, 5781 (2016)
H.Küpers et al, J. Cryst. Growth, 459, 43-49 (2017)

## Slide 9: Program package SilSim3D
A.N. Karpov, A.V. Zverev, A.G. Nastovjak, S.V. Usenkov, and N. L. Shwartz, Vychisl. Metody Programm., 15, 3, 388 (2014).
Input parameters of the model process:
- temperature T(K);
- flux intensity F(ML/s);
- duration (s)
Input parameters of the model system:
composition, crystal structure and orientation of the substrate;
initial layer morphology;
activation energies of possible elementary events (Eevent) .
Diamond-like crystal structure
Cyclic boundary conditions in the lateral directions

## Slide 10: Monte Carlo model
- Ga(s)
- As
- Ga(l)
l – liquid phase
s – solid phase
- As2
- mask film
(1) Ga and As2 adsorption
(2) As2 decay As2 → As + As
(3) As2 formation As + As → As2
(4) Particles diffusion
(5) Ga and As2 desorption
(6) As dissolution and diffusion through the liquid Ga droplet Ga(l)+As → As+Ga(l)
(7) Ga dissolution Ga(s)+Ga(l) → Ga(l)+Ga(l)
(8) GaAs crystallization Ga(l)+As → Ga(s)+As
(9) Mask etching by liquid gallium
Event probability:
9
4
A.N. Karpov, A.V. Zverev, A.G. Nastovjak, S.V. Usenkov, and N. L. Shwartz, Vychisl. Metody Programm., 15, 3, 388 (2014).
Program package
SilSim3D

## Slide 11: Simulation results
T = 890 K
FAs2 = 25 ML/s
FGa = 10 ML/s
S = 120×100 nm
3D view
Without As diffusion flow
With As diffusion flow

## Slide 12: Simulation results
T = 890 K
FAs2 = 25 ML/s
FGa = 5 ML/s
S = 120×100 nm
top views
3D view
time

## Slide 13: Crystallite formation model
GaAs(111)B
SiO2
Si
Ga
As2
GaAs(111)B
Ga
As2
GaAs(111)B
Ga
As2
GaAs(111)B
Ga
As2
GaAs(111)B
Ga
As2
t1
t2
t3
t4
t5

## Slide 14: Conclusions
Nanowire formation was demonstrated to be accompanied by the parasitic structure growth – massive GaAs clusters and tilted nanowires.
The qualitative model of GaAs cluster formation was proposed and proved by simulation.
During the growth process the growth conditions change: under high arsenic flux the first Ga droplets yield clusters, which collect part of the deposited material, so the subsequent Ga droplets are resulted in nanowire growth.
The self-catalyzed GaAs NW growth is a self-regulated process in which not only external fluxes determine arsenic and gallium flows to a catalyst drop, but these flows are also adjusted by the surface morphology.
ACKNOWLEDGEMENTS
Authors are grateful to T. Gavrilova for acquiring SEM micrographs.
This work was supported by RFBR (grant 18-02-00764)

## Slide 15: Thank you for your attention!

## Slide 16: Problem statement
Massive GaAs crystallites form between GaAs NWs
F.Bastiman et al, Nanotechnology 27, 095601 (2016)
F. Matteini et al. Cryst. Growth Des., 16, 5781 (2016)
H.Küpers et al, J. Cryst. Growth, 459, 43-49 (2017)
2 mm

## Slide 17: Experiment Nanowire growth
GaAs(111)B
tgr = 15 min
L ~ 1 mm, d ~ 30 nm.
NW density ~2·107 cm-2
GaAs(100)
tgr = 60 min
L ~ 6-8 mm, d ~ 90 nm.
NW density ~3·107 сm-2
L – NW length, d – NW diameter
3 mm