## Slide 1
-
III Международная конференция
Atomic structure of a single step and dynamics of Sn adatoms on the Si(111)--Sn surface
R.A. Zhachuk, D.I. Rogilo, A.S. Petrov, D.V. Sheglov, A.V. Latyshev, S. Colonna, F. Ronci
МОСКВА
25-27 ОКТ
Математическое моделирование в материаловедении электронных компонентов
2021
Methods: low-temperature scanning tunneling microscopy (LT-STM, Omicron), density functional theory calculations (SIESTA) using generalized gradient approximation (GGA).
References:
R. A. Zhachuk at al., Phys. Rev. B 104 (2021) 125437
F. Ronci et al., Phys. Rev. Lett. 95 (2005) 156101.
F. Ronci et al., Phys. Rev. Lett. 99 (2007) 166103.
F. Ronci et al., J. Phys.: Condens. Matter 22 (2010) 264003.
Atomic structure of a single step
Top view
Sideview
-Sn structure
Model “B”. Yellow balls – Sn atoms, R1, R2 – rest atoms, A1, A2 – Sn adatoms forming Sn chains along step edges, red, cyan and blue balls are Si atoms of the lower, middle and upper (111) terraces, respectively.
2) Proof: Lowest calculated surface energy among 50 tested models.
Sn-rich
Sn-depleted
1) Proof: STM images.
experimental
calculated
U>0
U<0
Dynamics of Sn adatoms at T=80 K
Constant current STM image
s-map: standard deviation of the current traces
Current traces
Calculated Potential Energy Surface (PES) for Sn atoms on the Si(111)- -Sn surface with steps: describes the energetics of adsorbed Sn atom on the reconstructed surface.
feedback loop is ON
feedback loop is OFF
feedback loop is OFF
The dynamics of Sn adatoms was detected near the steps (bright spots on the s-map ).
How does the double well look like?
PES
minima
Saddle
point
Top view
Sideview
-Sn
structure
Deepest PES minima
(double well)
Bright (dark) regions indicate energy
minima (maxima). The contour spacing is 0.2 eV. White circles are Si atoms; yellow circles are Sn atoms.
weak bond
Conclusions:
Step atomic structure is determined.
Dynamics of Sn adatoms near step edges is explained by formation of double wells.